## Slide 1
Metal Cutting Processes
  Flexible Manufacturing

## Slide 3: Oxygen Acetylene Cutting
  Oxygen Acetylene Cutting: the use of a torch fueled with oxygen and acetylene to heat the metal and blow the molten metal from the cut

## Slide 4: Plasma Cutting
  Plasma Cutting: the use of a blast of air or some other gas to super heat the metal and force it from the cut

## Slide 5: Dross
  Dross: the scum that forms on the surface of molten metal or the slag from cutting metal

## Slide 6: Plasma
  Plasma: the fourth state of matter; a highly ionized gas

## Slide 7: Oxygen Acetylene vs. Plasma Cutting
Oxygen Acetylene Cutting | Plasma Cutting
Heats then oxides metal | Super heats and blows metal from cut
Cuts only ferrous metal | Cuts all conductive metal including aluminum and stainless steel
Cuts thicker metal | Cuts faster
Leaves large amounts of dross | Leaves little or no dross

## Slide 8: Oxygen Acetylene Cutting Parts
Oxygen Tank
Oxygen Regulator Adjusting Screw
Safety Chain
Acetylene Regulator Adjusting Screw
Acetylene Regulator
Acetylene Tank
Gas Lines
Cart
Oxygen Regulator

## Slide 9: Oxygen Acetylene Regulators
Line Pressure Gauges
Regulator Adjusting Screws
Acetylene Regulator
Acetylene Tank
Gas Lines
Bottle Pressure Gauges
Oxygen Regulator

## Slide 10: Oxygen Acetylene Cutting Torch Parts
Oxygen Valve on Handle
Acetylene Valve on Handle
Cutting Torch Head
Oxygen Blast Trigger
Cutting Head Oxygen Valve
Torch Handle

## Slide 11: Oxygen Acetylene Cutting Setup
  Begin the Oxygen Acetylene Cutting by setting the regulators. Open the torch handle oxygen valve all the way. Open the cutting head oxygen valve one turn.
Open all the way
Open one turn

## Slide 12: Oxygen Acetylene Cutting Setup
  Adjust the pressure on the regulator to a line pressure of 30 lbs. Close the cutting torch oxygen valve.

## Slide 13: Oxygen Acetylene Cutting Setup
  Open the acetylene tank valve a 1/4 turn. This is a safety factor. If something happens, you can turn the fuel off quickly.
Tank Valve

## Slide 14: Oxygen Acetylene Cutting Setup
  Open the acetylene valve on the torch handle a 1/4 turn. Adjust the line pressure on the gauge to 5 PSI. Use the adjusting screw to set the pressure. Close the torch handle valve.
Line Pressure Gauge

## Slide 15: Oxygen Acetylene Cutting Setup
  Open the acetylene valve on the torch handle. Use a spark igniter to light the torch. Open the oxygen valve after the torch is lit and adjusted to a neutral flame. This flame has a bright blue flame with no light blue feathering outside the main flame.
Feathered Flame
Neutral Flame

## Slide 16: Oxygen Acetylene Cutting Setup
  Place the cutting tip about 1/8 inch away from the metal to be cut. Heat the metal to a bright red, then press the oxygen blast trigger.

## Slide 17: Oxygen Acetylene Cutting Operation
  The oxygen blast will increase the metal’s temperature to a molten state and it will blow the metal from the cut. Keep the torch in a vertical position and follow your guide.

## Slide 18: Oxygen Acetylene Cutting Operation
  Move the cutting torch at a speed that will keep the molten metal puddle intact. If the torch is moved too fast, the metal will not be heated properly and the cutting will stop. Close the oxygen blast trigger and let the metal reheat to a bright red, then restart the cut.

## Slide 19: Oxygen Acetylene Cutting Operation
  At the end of the cut, tilt the torch a little to cut through the bottom of the metal. A steady movement will produce a straight cut. An unsteady movement will produce a wavy cut.
  When finished cutting with the torch, close the oxygen valve on the torch handle first. Then close the acetylene valve. This safely stops the flame.
Oxygen Valve
Acetylene Valve

## Slide 20: Oxygen Acetylene Cutting Operation
  The turning off of the cutting torch when completely finished is the same process as when welding or brazing. The main valves on the tanks will be closed. After closing both tank valves, open the acetylene valve on the handle to bleed the acetylene line from the tank to the torch. The regulator will show 0 pressure on the gauges. Close the acetylene valve on the torch and unscrew the regulator adjusting screw.
  After the acetylene line is drained or purged, do the same thing to the oxygen line. Open the oxygen valve on the torch handle and drain the oxygen from the line and regulator. When the gauges read 0 pressure, loosen the regulator adjustment valve. Close the oxygen valve on the torch handle and the cutting head. Take the torch and other items to their storage place and straighten the hoses.

## Slide 21: Plasma Cutting Torch

## Slide 22: Plasma Cutting Power Supply Parts
Ground Clamp
Air Pressure Gauge
Air Pressure Control
Machine Lights
Connection for Torch
Amperage Control

## Slide 23: Plasma Cutting Torch Parts
Trigger Lock
Trigger
Handle
Cutting Tip

## Slide 24: Plasma Cutting Operation
  Place drag shield directly on the metal. The arc should be pointed straight down.
  Raise the trigger lock and press the trigger. This starts the pilot arc. Igniting the plasma arc occurs when the torch is placed on the metal.
  Place drag shield directly on the metal. The arc should be pointed straight down.
  Raise the trigger lock and press the trigger. This starts the pilot arc. Igniting the plasma arc occurs when the torch is placed on the metal.

## Slide 25: Plasma Cutting Operation
  When the cutting arc starts, move tip slowly over across the metal.
  Adjust the cutting speed across the metal so the sparks go through the metal and out the bottom of the cut.

## Slide 26: Plasma Cutting Operation
  When ending the cut, tilt the torch up, and cut the back corner of the plate. This makes a cleaner cut.
  Release the trigger when the tip leaves the metal. The torch will go into cool down mode and air will flow around the electrode. Pressing the trigger again will restart the arc.

## Slide 27: Cutting Projects

## Slide 28: Cutting Projects Assignments
You will choose a project to weld. The plans and instructions can be picked up from the teacher.
REQUIRED:
Cutting Process Basic Assignment
OPTIONAL:
Receiver Hitch Tube Cover
Address Boot Scraper

## Slide 29: Cutting Process Basic Assignment

## Slide 30: Cutting Process Basic Assignment
CUTTING PROCESS BASIC ASSIGNMENT
1
NAME
DATE
1/4” THICKNESS PLATE 4” X 6”
USE A TORCH AND CUT THE DASH LINES
1 1/2” DIA.
1” DIA.
1/2” DIA.
3/4” DIA.
1” RADUS
4”
6”
4 CUTS 3 1/2” LONG

## Slide 31: Cutting Process Basic Assignment Rubric
Visual Inspection | Fail | Pass | Points Awarded | Comments
Straight cuts | 0 Points | 1 -10 Points |  | 
Straightness | 0 Points | 1 -10 Points |  | 
Cut through | 0 Points | 1 -10 Points |  | 
Excess dross | 0 Points | 1 -10 Points |  | 
Holes | 0 Points | 1 -10 Points |  | 
Size | 0 Points | 1 -10 Points |  | 
Circle shape | 0 Points | 1 -10 Points |  | 
Edge cuts | 0 Points | 1 -10 Points |  | 
Smoothness | 0 Points | 1 -10 Points |  | 
A=80-90 B=70-79 | C=60-69 | D=50-59 Total: |  | 

## Slide 32: Receiver Hitch Tube Project

## Slide 33: Receiver Hitch Tube Project

## Slide 34: Texas Hitch Cover

## Slide 35: Other Hitch Cover Suggestions

## Slide 36: Receiver Hitch Tube Project Rubric
Visual Inspection | Fail | Pass | Points Awarded | Comments
Design | 0 Points | 1 -10 Points |  | 
Straightness | 0 Points | 1 -10 Points |  | 
Smoothness | 0 Points | 1 -10 Points |  | 
Excess dross | 0 Points | 1 -10 Points |  | 
Hole | 0 Points | 1 -10 Points |  | 
Size | 0 Points | 1 -10 Points |  | 
Edge cuts | 0 Points | 1 -10 Points |  | 
Weld | 0 Points | 1 -10 Points |  | 
A=70-80 B=60-69 | C=50-59 | D=40-49 Total: |  | 

## Slide 37: Address Boot Scraper

## Slide 38: Address Boot Scraper
501
1/4” x 4” WIDE PLATE
8” to 12” LONG
ADJUST FOR ADDRESS
1/2” DIA. X 12” LONG HOT ROLLED RODS

## Slide 39: Address Boot Scraper Rubric
Visual Inspection | Fail | Pass | Points Awarded | Comments
Design | 0 Points | 1 -10 Points |  | 
Straightness | 0 Points | 1 -10 Points |  | 
Smoothness | 0 Points | 1 -10 Points |  | 
Excess dross | 0 Points | 1 -10 Points |  | 
Hole | 0 Points | 1 -10 Points |  | 
Size | 0 Points | 1 -10 Points |  | 
Edge cuts | 0 Points | 1 -10 Points |  | 
Weld | 0 Points | 1 -10 Points |  | 
A=70-80 B=60-69 | C=50-59 | D=40-49 Total: |  | 

## Slide 40: Personal Protective Equipment
  Welding goggles or hood
  Gloves
  Safety glasses when not wearing welding goggles or hood